## Slide 1: P4 – The Key to Success! DirectFET Boardmount: The Fundamentals
June 2008
Notes: <number>
7

## Slide 2: P4 - The Key To Success !
Pads
Paste
Pick & Place
Profile

## Slide 3: P1 - Pads
Ensure that the pad outline on the board matches the recommendations by International Rectifier for the DirectFET outline being used.
Get it from Application Note AN1035 on www.irf.com
Please note that it is critical that the pad outlines on the board are checked as boards delivered from PCB vendor may differ from original gerber design files

## Slide 4: P2 - Paste
Solder Paste Volume is critical to solder joint quality and production yields.
Ensure the ratio of solder paste volume to PCB pad area is correct.
Get it from Application Note AN1035 on www.irf.com

## Slide 5: P3 – Pick & Place
In order for all DirectFET solder connections to be made, the Pick & Place machine should be set to give a placement force of 150 – 250g
and/or
an overtravel into the printed solder paste of 0.05 – 0.10mm
(0.002 – 0.004”)

## Slide 6: P4 - Profile
Ensure that the temperature profile seen by the DirectFET meets at the least the minimum profile requirements as specified by the solder paste vendor.
Temperature profile of the DirectFET must be measured underneath / at the DirectFET with a thermocouple ‘buried’ in the board.
Thermocouple

## Slide 7: P4 - Profile
DirectFET devices are not sensitive to Reflow Profile.
However, due to the superior heatsinking properties of the device, it is important to understand what thermal profile the DirectFETs see during the Reflow Process. Therefore, it is vital to measure the Reflow Profile AT THE DIRECTFETS, and apply the Reflow Profile Specification as laid out in the solder paste vendors Technical Datasheet for the Solder Paste being used.